## Slide 1
WP3: Hybrid metrology and modeling
Aim is to develop data interpretation methods for quantifying the material quality of WBG semiconductor wafers that can be applied using fast and large-area characterisation techniques.
This will be achieved by bringing together the complementary techniques developed in WP1 and WP2, performing
data fusion and supporting combined uncertainty estimation using analytical and numerical modelling.
Main outputs:
D1 (M15, lead PTB): ‘Report on capabilities and limitations of advanced sampling strategies and compressed sensing for spatially-resolved and spectrally-resolved metrology of wide bandgap semiconductors. Instrumentation requirements to achieve < 10 % uncertainty in measurement of defect density using these measurement strategies will be identified’.
D4 (M36, lead CMI): ‘Uncertainty budget and dataset demonstrating high-throughput measurements with < 10 % uncertainty in defect density using compressed sensing and data fusion methods’

## Slide 2
Task 3.1: Novel sampling strategies for high-resolution and large-area measurements
Aim is to develop sampling methods for large area and high resolution measurements, namely for optical methods, including both sampling in space and in the spectral domain.
Involved partners: CMI, PTB, NPL and BAM
Activities done in the first year:
Deliverable D1 was completed.

## Slide 3
Tasks 3.2 and 3.3: Numerical modelling and hybrid metrology
Task 3.2: Numerical modelling for data interpretation across different length-scales
Aim is to develop numerical models to address specific problems in wafer scale inhomogeneities measurements using different techniques:
- optical models for local scattering and its far-field signatures (TU Delft, NPL)
- tip-sample interaction in near-field optical spectroscopy (PTB, CMI, NPL)
- density of SiC/SiO2 interface defects in near-field and far field optical methods (BAM, PTB, NPL, TUBITAK)
Activities were mostly presented on M27 meeting.

## Slide 4
Tasks 3.2 and 3.3: Numerical modelling and hybrid metrology
Task 3.3: Hybrid metrology methodologies to evaluate material quality parameters
Aim is to use hybrid metrology approach to evaluate data from WP1 and WP2, combining methods using different principles and different spatial resolutions:
- comparing near-field and far-field scattering data to detect defects on known samples (NPL, TU Delft, PTB, Aixtron),
- combining scatterometry, ellipsometry and PL mapping to characterize wafer-scale defects (PTB, TU Delft, NPL, BAM, TUBITAK, CMI),
- comparing TERS and ellipsometry on defects on SiC samples with different oxide layers (BAM, PTB, NPL, TU Wien),
- combining data from KPFM and cathodoluminescence (CEA, NPL, CMI),
- combining PL mapping and SPM for sub-surface defect density measurements (PTB, NPL, CMI),
- determining uncertainties for the above data fusion methods.

## Slide 5
Tasks 3.2 and 3.3: Numerical modelling and hybrid metrology
Initial measurements on the same samples were performed, can we get some conclusions?
Do we need more detailed protocol for measurements, to make them comparable?
A plan how to further circulate samples and how to evaluate the data?

## Slide 6
Compressed sensing routines for Gwyddion
A3.1.3: CMI, with support from NPL and PTB will create a subset of the compressed sensing
data processing techniques developed in A3.1.2 suitable for SPM method and will
implement it into open source software Gwyddion.
CMI custom software tool for GP prediction:
Can be considered a form of supervised machine learning, can handle data of arbitrary dimension (2D in our case of image data)
Assuming both inputs and outputs normally distributed, allow straightforward and understandable computer implementation using just basic computing libraries (linear algebra, minimization)
After training can predict mean value (not used with our method) as well as variance/uncertainty thereof (base for our method)

## Slide 7
Compressed sensing routines for Gwyddion
CMI custom software tool was further developed:
underlying computation library (based on open-source GPF project) already fairly optimized
Training + candidate selection (requiring pause during scanning): <10 s for the first 5 steps (512x512px image, 16 lines scanned in each step, 8px spacing between training points, 4x excess factor for candidate line number generation and evaluation)
Paper in preparation.
New mode being added for prediction with point-based measuring mode (i.e., when single-point acquisition relatively expensive compared to movement, e.g. thermal/mechanical measurements)

## Slide 8
Compressed sensing routines for Gwyddion
9 (initial scan)
17
25
33
No. lines scanned
Scanned data
Pred. uncertainty (logscale) to identify regions of interest
Newly scanned lines eliminate regions of greatest uncertainty

## Slide 9
Compressed sensing routines for Gwyddion
Newly scanned lines eliminate regions of greatest uncertainty
No. lines scanned
Scanned data
Pred. uncertainty (logscale) to identify regions of interest
41
49
512 (complete image)

## Slide 10
A3.2.2, A3.3.2 Near-field simulations at CMI
Some activities in the project are related to near-field simulations on defects.
A3.2.2: near-field microscopy data interpretation
A3.3.2: optical data interpretation for spatial map of defects
Gsvit: open source software for FDTD modeling http://gsvit.net
General FDTD package optimized to include various imperfections, like roughness, suitable for Monte Carlo calculations.
More suitable for non-periodic structures than RCWA, simpler setup for general 3D models than FEM. Less accurate than FEM due to staircasing effects and computationally ineffective mesh refinement.
New computing cluster at CMI from Sep23: 1280 AMD Epyc 3 cores, 10 TB RAM for parallel workload
+ 1x 128-core / 4 TB RAM large-memory node + plus 1x NVidia Tesla A100 (870 GB) for GPU-based computations & AI

## Slide 11
A3.2.2, A3.3.2 Near-field simulations at CMI
Testing GSvit suitability for CFS calculations
(also for Polight project, when related to gratings)
Finalized simple CMI setup for CFS, goal was to understand better the method.
Primary goal was to measure non-periodic structures, however we found that for newcomers it is not ideal.
GSvit calculations developed in parallel, presented on last meeting, now focusing namely on speed and accuracy.

## Slide 12
A3.2.2, A3.3.2 Near-field simulations at CMI
Testing the FDTD performance on more complex but still periodic structures.
Further inputs for comparison to FEM obtained from TU Delft during and after Nanoscale conference.

## Slide 13
A3.3.4 KPFM uncertainties
A3.3.4 CEA will develop and demonstrate a data fusion method combining KPFM and cathodoluminescence results (A2.3.1) in order to achieve < 10 % uncertainty in defect density characterisation. NPL and CMI will contribute to demonstration of KPFM signal uncertainty based on results of A2.3.2.
Uncertainty components measured using various samples (Budgetsensors two metal sample, Bruker KPFM test sample, set of 4 metallic layers, HOPG, resolution test two metal sample).
Draft for a pilot comparison study developed together with NPL.
NPL measured a set of samples and sent it to CMI.
1
2
3
4

## Slide 14
A3.3.4 KPFM uncertainties
Measurements for KPFM comparison: sample E8, G11

## Slide 15
A3.3.4 KPFM uncertainties
Measurements for KPFM comparison: sample G12
Budgetsensors sample and HOPG as a reference, between all measurements.
AM-KPFM and partly FM-KPFM.
Location of same areas as measured by NPL (10x10) is not easy,
either larger areas or more detailed search needs would be necessary.

## Slide 16
D4: data fusion in Gwyddion
Related to D4, we would like to test our correlative data interpretation capabilities on the datasets measured in the project. This means loading data from different measuring techniques into Gwyddion, registering, rotating and resampling them to fit pixel-by-pixel.
The possible data combinations to be loaded and processed same way:
- NPL Raman maps and CMI large area KPFM data
- ellipsometric data and AFM topography?
- PL maps and AFM topography?
A combination of volume data and 2D data can be processed together using new arithmetic modules, however, the real data analysis that could be somehow useful still needs to be discussed.

## Slide 17
Far- to Near-Field Relation in Ga2O3 -> Application to SiC

## Slide 18
s-SNOM modelling
Get bulk optical properties from far-field measurements
s-SNOM modelling workflow
Plug them into a model of tip + sample
Our FEM-model
Reference to known material
Remove background through third order harmonic detection
Place the detector

## Slide 19
Verification on Si
Permittivity
Finite Dipole Model (FDM)
Finite Element Method (FEM)
FEM approach improves description of measured data compared to widely used Finite Dipole Model
A. Cvitkovic, et al. Opt. Express 15, 8550–8565 (2007)

## Slide 20
Application to SiC
Strong resonators like SiC more challenging
Qualitative agreement, but quantitative differences to the FDM

## Slide 21
Application to complex structures
AAA
M
ABA
M
M
ACA
M
M
ADA
Free nanoparticle  Single resonance
Metallic substrate  Two resonances
Core-shell NP on substrate  strong resonance enhancement
Core radius change  spectral shift
Variable material ()
Metallic material
Nanoparticle as a complex, defect-like structure

## Slide 22: Activities TU Delft WP3
Shape retrieval of structures using Coherent Fourier scatterometry
Silvania Pereira, Anubhav Paul and Sarika Soman

## Slide 23: Subwavelength shape retrieval
Physical model
18-01-2024
FDTD numerical model
Fourier plane (Far-Field) is imaged in the CCD camera.

## Slide 24: Subwavelength shape retrieval
We aim to distinguishing between three types of structures i.e., a cube, a cylindrical pillar, and a triangular pillar with the help of different illumination schemes.
For structures having dimensions smaller than 100 nm we cannot distinguish between the two cases at wavelength of 405 nm.
Triangular structure has a large variation in correlation implying that it has the largest influence on the different polarization states.
We observe that for cube and cylinder, the correlation is always 1, this is because structure is symmetric across both the polarization states.
When we rotate the cube and break this symmetry, we observe deviation of correlation from 1.
The correlation between the far-fields of TE and TM polarized
illumination on structures of the same shape and dimensions.
18-01-2024
a
a
a
a
a
a
b
a

## Slide 25: Subwavelength shape retrieval
We rotate the cubic structure across 0 to 2 and correlate the far-fields with that of the nonrotated cube.
We observe a periodic variation dependent on the symmetry of the structure. (a cube has a rotational symmetry after every π/2 rotation and so does the curve)
By rotating the sample from 0 to 2 and analyzing the period of the correlation curve we can determine whether the shape is a triangle, square, circular, pentagon, etc.
The correlation between the far-fields of different structures. This was done for TM polarized incident beam and the x-axis denotes the degree of rotation.
18-01-2024

## Slide 26
We fabricated samples (Si on Si) with pillars of different shapes and sizes:
Circular, square, rectangles and triangular lateral shapes, fixed height
Sizes range from 1 micron to 100 nm

## Slide 27
t=0
t=30
t=60
t
0.55NA
0.9NA
Preliminary results: triangular structure

## Slide 28
Corr2(t0,t0)=1
Corr2(t0,t30)=0.8038
Corr2(t0,t60)=0.6881
Correlation as a function of the rotation angle

## Slide 29: Activities TU Delft WP3
Simulation work has been presented in 2 conferences:
NWO Physics in Veldhoven, The Netherlands (national)
Nanolight 2024 in Spain
We had interactions with CMI to check the FDTD modelling of the interaction of the focussed field with the nanostructure